## Slide 1
Scanning probe microscopy (SPM) and lithography
Atom and particle manipulation by STM and AFM.
AFM oxidation of Si or metals.
Dip-pen nanolithography (DPN).
ECE 730: Fabrication in the nanoscale: principles, technology and applications
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Nanofabrication: principles, capabilities and limits, by Zheng Cui

## Slide 2
STM Lithography:
Atomic scale patterning technique
Manipulation of both single atoms or molecules
Can be used, for example, quantum data storage with extremely high storage density (one atom per bit).
Pushing/pulling atoms using STM
Atom movement mechanism:
When lateral force Fx exceeds the hopping barrier, the atom jumps to the adjacent row.
High electric field polarizes the molecule and may make it jump from the surface to the tip or tip to the surface.
However, this might not be well controllable, then one should avoid too high electric field (so atom remains close to substrate surface all the time) and use attractive van der Waals force to pull the atoms.
Hla et al., Phys. Rev. B 67, 201402 (2003)

## Slide 3
Diffusion of atoms

## Slide 4
Atomic manipulation by STM
M.F. Crommie, C.P. Lutz, D.M. Eigler. Science 262, 218-220 (1993)
Circular corral (radius 71.3Å), 48 Fe atoms on copper (111).
Quantum-mechanical interference patterns

## Slide 5
STM nano-patterning at IBM
The presence of a quantum mirage might be used to represent one bit of data in a region far smaller than any current electronic device can manage.
M.F. Crommie, C.P. Lutz, D.M. Eigler, Science 262, 218-220 (1993).
M.F. Crommie, C.P. Lutz, D.M. Eigler, Nature 363, 524-527 (1993).

## Slide 6
Title : The Beginning Media : Xenon on Nickel (110)
Title : Stadium Corral
Media : Iron on Copper (111)
More STM nano-patterning at IBM

## Slide 7
Manipulation of nanoparticles by AFM

## Slide 8
Manipulation of nanoparticles by AFM

## Slide 9
AFM manipulation of carbon nanotube
IBM nanotube manipulation for position nanotube on transistors.

## Slide 10
Scanning probe microscopy (SPM) and lithography
Atom and particle manipulation by STM and AFM.
AFM oxidation of Si or metals.
Dip-pen nanolithography.

## Slide 11
AFM oxidation mechanism
Voltage bias between a sharp probe tip and a sample generates an intense electric field at the tip, which leads to oxidation of silicon or anodization (oxidation) of metals. This is an electrochemical process.
The high field desorbs the hydrogen on the silicon surface and enables exposed silicon to oxidize in air (the oxidation rate is enhanced by the presence of the accelerating field).
That is, the negatively biased tip induces a high electric field which ionizes the water molecules from the ambient humidity between the tip and the substrate to produce OH- ions that act as an oxidant.
The electric field enhances the vertical drift of these ion species away from the tip towards the surface where they react with underlying atoms to form a localized oxide beneath the tip.
Since the oxidation process requires an electrical current, both the tip and substrate must have some conductivity.

## Slide 12
De-passivation of Si:H by STM
STM image of a Si(100)–21–H surface. M corresponds to a STM induced hydrogen desorption obtained with a constant current of 2nA, an electron dose of 410-4 C/cm, and a sample bias voltage of 6V.
Hydrogen desorption yield as a function of the sample bias voltage.
H- terminated Si resulted from HF etch of Si whose top surface (2nm) is usually oxidized in air.
Syrykh, “Nanoscale desorption of H-passivated Si.100.–231 surfaces using an ultrahigh vacuum scanning tunneling microscope”, JAP, 85, 3887-3892 (1999).

## Slide 13
Resulting oxide affected by experimental parameters
    Voltage (typically from 5-10V)
    Tip Scan Speed (stationary to tens of µm/s)
    Humidity (20% to 80%)
Detected current can be used for process control
Changes in translational velocity influence current flow
AFM oxidation

## Slide 14
Silicon dioxide line on silicon written & profiled by AFM
Silicon dioxide line on silicon written by AFM oxidation
Though the height is only 1nm, it is enough to etch deep into Si using hot KOH solution. The etching selectivity (Si:SiO2) is 1000:1.

## Slide 15
Produced by chemical etching of AFM written lines
Etching into Si by KOH using SiO2 as mask
However, such high aspect ratio anisotropic vertical etching can only be achieved along certain directions ((111) plane) on (110) Si wafer.
(111) plane
(111) plane

## Slide 16
AFM tip-induced Si oxidation structures patterned on Si substrate with applied DC voltage from -3 to -9V and 500ms at 60% ambient humidity. Minimum features size 10nm.
AFM oxidation: dependence of voltage
A. Tseng and A. Notargiacomo, J. Nanosci. Nanotechnol. 5, 683 (2005).

## Slide 17
Ph. Avouris et al, App. Phys. A 66, S659 (1998)
AFM oxidation on Si
Oxide height depends on voltage and time.
Oxidation and HF etch can also occur simultaneously by carrying out AFM oxidation in diluted HF solution. This way one can achieve arbitrary deep holes by fixing the tip at one location for extended time.

## Slide 18
Nano-oxidation on SOI wafer
Besides crystalline and SOI silicon, oxidation can also be performed on amorphous Si.

## Slide 19
V.B. et al. Microelectronic Engineering, Vol. 61-62 (1) (2002) pp. 517-522
Nano-FET by AFM oxidation on SOI wafer
FET: field effect transistor
SOI: silicon on insulator (SiOx)

## Slide 20
AFM oxidation of III-V semiconductors
High mobility two-dimensional electron gas (2DEG)
below sample surface
Matsumoto et al., APL 68, 34 (1996); Held et al., APL 73, 262 (1998)
Direct patterning of AlGaAs/GaAs

## Slide 21
AFM anodization of GaAs
Quantum ring with Coulomb blockade
Fuhrer, “Energy spectra of quantum rings”, Nature, 413, 822-825 (2001)

## Slide 22
Scale up using tip array

## Slide 23
50  1 parallel lithography over 1cm  1cm
50 parallel AFM tips oxidizing (100) silicon. The pattern is then transferred to the bulk Si using KOH etch.
The lines are on a 200m period, the cantilever’s spacing.
The blue box in the bottom left represents the scan area of a typical AFM.

## Slide 24
Scanning probe microscopy (SPM) and lithography
Atom and particle manipulation by STM and AFM.
AFM oxidation of Si or metals.
Dip-pen nanolithography.

## Slide 25
Dip pen nanolithography (DPN)
Revolutionary science developed at Northwestern University
Allows for deposition of inks, including DNA, at nm resolution
For ultra-high-density gene chips with direct write of DNA onto substrate
Chad Mirkin (Northwestern)

## Slide 26
Scanning probe-based lithography technique using probe tip like a pen.
Tip is dipped in chemical “ink” and transfers nanoparticles, biomolecules, etc. to substrate through contact “writing”.
In a high-humidity atmosphere, a nanoscale water droplet condenses between the AFM tip and the substrate.
The drop of water acts as a bridge over which the ink molecules migrate from the tip to the substrate surface where they are deposited.
Demonstrated resolution: 15nm.
Dip-pen nanolithography (DPN)
By far DPN is the most widely used SPM-based patterning techniques, because other methods (e-beam lithography, FIB, photolithography…) cannot handle liquids that is important for chemical and bio-applications.
The competing technique is micro-contact printing (faster, lower resolution).
It is still used for research, not for production.
DPN is commercialized by NanoInk founded by Mirkin.

## Slide 27
Ultra-high resolution pattern of mercaptohexadecanoic acid on atomically-flat gold surface.
DPN generated multicomponent nanostructure with two aligned alkanethiol patterns.
Richard Feynman's historic speech written using the DPN nanoplotter.
Dip pen nanolithography patterns

## Slide 28
Science, Vol 295, Issue 5560, 1702-1705, 1 March 2002
Protein patterning by DPN
MHA: mercaptohexadecanoic acid

## Slide 29
Direct-Write DNP for protein array
Rabbit anti-body IgG assembled on an MHA dot array by DPN.
After treatment with a solution containing lysozyme, goat/sheep anti-IgG, human anti-IgG, and rabbit anti-IgG;
A control protein nano-array
After exposure to a solution containing lysozyme, retronectin, goat/sheep anti-IgG, and human anti-IgG (no change).
Height profiles of TM(tapping mode)-AFM images

## Slide 30
Ultrahigh density DNA arrays
fluorescent image
Protein nanostructures
Virus nano-arrays
Bio-matter patterning by DPN

## Slide 31
Etch barrier templates for solid-state nanostructures
This application (SAM plus wet-etch) is the classical application for micro-contact printing.
SAM (self assembled mono-layer)

## Slide 32
Hard material patterning by DPN (plus wet-etch)
Silver nanostructures
Gold Nanostructures
Single nanoparticle lines
Sol-gel materials (>100 different oxides can be patterned)
Silicon nanostructures
Gold nano-gap on Si/SiO2
Probably no wet-etch

## Slide 33
Thermal DPN
Nelson and King, “Direct deposition of continuous metal nanostructures by thermal dip-pen nanolithography”, APL, 2006.
Conventional DPN:
Dynamic control difficult, unable to “turn-off” deposition quickly, causing contamination and smearing.
Metrology not possible without unintended deposition or prior cleaning of probe tip
Thermal DPN:
Heating element integrated into cantilever
Allows use of “inks” that are solid in ambient conditions (become liquid at high T)
Deposition easily turned on/off by modulating heating element
Surface imaging possible without smearing/contamination

## Slide 34
Thermal time constant of 1-10μs.
Temperature sensitive cantilever resistance (2-7k for 25-550°C) used for calibration.
Indium as deposition metal (melt @ 156.6°C).
Loading: indium substrate scanned with 500nN contact force with tip temperature of 1030°C (heat loss to substrate and surrounding In film important).
Continuous lines deposited by reheating cantilever while contacting substrate.
Dimensions depend on tip loading, temperature, speed, and repetitions.
Successful deposition for: 250-800°C, 0.01-18μm/s, 32-128 raster scans, on borosilicate glass, quartz and silicon substrates.
Deposited pattern: 50-300nm wide, 3-12nm high.
Can be used like nano-soldering for circuit repair.
Thermal DPN

## Slide 35
Nanoscale dispensing
Pattern liquids, e.g. biomolecules, suspensions, by surface chemistry.
Parallel probes for multi-material deposition.
Integration of fluidic system possible.
Tip can be fabricated by FIB milling
Glycerol on SiO2, image size 10μm x 10μm
dots size 50–100nm

## Slide 36
DPN applications
International Institute for Nanotechnology
Northwestern University

## Slide 37
One application: cancer diagnosis using tumor markers
Tumor marker:
Found in the blood, other body fluids, or tissues.
High level of tumor marker may mean that a certain type of cancer is in the body.
Examples of tumor markers include CA 125 (ovarian cancer), CA 15-3 (breast cancer), CEA (ovarian, lung, breast, pancreas, and gastrointestinal tract cancers), and PSA (prostate cancer).
Currently, the main use of tumor markers is to assess a cancer's response to treatment and to check for recurrence.
Scientists continue to study these uses of tumor markers as well as their potential role in the early detection and diagnosis of cancer.
Mirkin, “Multiplexed Detection of Protein Cancer Markers with Biobarcoded Nanoparticle Probes”, JACS, 2006.

## Slide 38
A dip-pen nanolithography that has an array of 55,000 pens that can create 55,000 identical patterns.
However, here each pen is not individually and independently addressed/controlled, which is not necessary when writing identical arrays (though some tips may hit the surface and get damaged due to lack of feedback).
Parallel dip-pen nanolithography
The background shows some of the 55,000 miniature images of a 2005 US nickel made with dip-pen lithography. Each nickel image with Thomas Jefferson's profile (in red) is made of a series of 80nm dots. The inset (right) is an electron microscope image of a portion of the 55,000-pen array.
Mirkin, “Massively parallel dip-pen nanolithography with 55 000-pen two-dimensional arrays”, Angewandte Chemie International Edition, 2006

## Slide 39
DPN is a unique scanning-probe-based lithographic tool for generating high-resolution patterns of chemical functionality.
The combination of resolution, registration, and direct-write capability offered by DPN distinguishes it from any alternative lithographic strategy and makes DPN a promising tool for patterning soft organic and biological nanostructures.
More efforts should be put in improving the speed and in transforming it into massively parallel process to be a powerful production tool in life science.
Summary for DPN
Single crystal silicon probes