## Slide 1
Chapter 1 Introduction and Historical Perspective
Introduction.
Growth of IC – Moore’s law.
Some history in IC industry.
Semiconductors.
Semiconductor devices, semiconductor technology families.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Silicon
“Diamond” structure
Si # density:
8/(5.43Å)3=51022cm3

## Slide 3
Carrier concentrations of intrinsic (undoped) Si
1.12eV >> kT =0.026eV for T=300K, so ni is very low at room temperature.
Temperature in K
ni (cm-3)
n=p=ni
Notes: From the right figure, bandgap for Ge is higher or lower than Si? How about GaAs?

## Slide 4
Doping of silicon
Adding parts/billion to parts/thousand of “dopants” to pure Si can change resistivity by 8 orders of magnitude !
The key to building semiconductor devices and integrated circuits lies in the ability to control the local doping and hence local electronic properties of a semiconductor crystal.
1m = 100 cm

## Slide 5
Doping of silicon
By substituting a Si atom with a special impurity atom (Column V for donor, Column III for acceptor), a conduction electron or hole is created.
Semiconductor with both acceptors and donors has 4 kinds of charge carriers
Mobile, contribute to current flow when electric field is applied.
Immobile, DO NOT contribute to current flow with electric field is applied. However, they affect the local electric field

## Slide 6
Energy band description of electrons and holes contributed by donors and acceptors
EC = bottom of conduction band
EV = top of valence band
ED = Donor energy level
EA = Acceptor energy level
At room temperature, the dopants of interest are essentially fully ionized.

## Slide 7
Intrinsic and extrinsic silicon
Intrinsic: un-doped, or doping level lower than ni.
Extrinsic: carrier density determined/controlled by doping level.
For semiconductor device, it is usually extrinsic at room temperature.
But the semiconductor often becomes intrinsic at device fabrication temperatures (e.g. oxidation is done at >900oC).
Approximate definition of doping levels:
N-- or P-- : ND or NA < 1014 cm-3
N- or P- : 1014 cm-3 < ND or NA < 1016 cm-3
N or P : 1016 cm-3 < ND or NA < 1018 cm-3
N+ or P+ : 1018 cm-3 < ND or NA < 1020 cm-3
N++ or P++: ND or NA > 1020 cm-3
Si # density : 51022 cm-3
Intrinsic Si at RT: ni=1.45 1010 cm-3

## Slide 8
Electron and hole concentrations for homogeneous semiconductor
n: electron concentration (cm-3)
p : hole concentration (cm-3)
ND: donor concentration (cm-3)
NA: acceptor concentration (cm-3)
Charge neutrality: ND+ + p = NA- + n
At thermal equilibrium, np = ni2
(for intrinsic semiconductor n=p=ni, so np=ni2. This same relation also holds for extrinsic case)
Note: Carrier concentrations depend on NET dopant concentration (ND - NA)!
Therefore: p-type doping can be realized on n-type substrate if NA > ND, and vice versa.

## Slide 9
Fermi level and carrier concentration
The probability of an electron occupying any particular energy level E is given by:
F(E) = [1 + exp((E-EF)/kT))]-1  exp(-(E-EF)/kT) for E > EF + a few kT.
The probability of an electron not occupying any particular energy level E, or the probability of finding a hole there, is given by:
1 - F(E) = 1 - [1 + exp((E-EF)/kT))]-1  exp(-(EF-E)/kT) for E < EF - a few kT.
me,h* is density of states effective mass.
For Si at RT, NC = 2.81019cm-3, NV = 1.041019cm-3

## Slide 10
Carrier drift and carrier mobility
When an electric field is applied to a semiconductor, mobile carriers will be accelerated by the electrostatic force.
This force superimposes on the random thermal motion of carriers:
E.g. electrons drift in the direction opposite to the E-field.
Average drift velocity = |v| = μE,  is carrier mobility.
Electron current density: Jn = (-q)nvn = qnnE, n is free electron concentration.
Hole current density: Jp = (+q)pvp = qppE, p is hole concentration.
Total current density: J = Jn + Jp = E, conductivity  = (1/) = qnn + qpp
 is resistivity. Usually either n or p dominates. E.g. if n >> ni, then p = ni2/n << ni.
For Si at RT, with low doping concentration and small fields, maximum values:
n = 1500cm2/Vsec; p = 500cm2/Vsec < n, so NMOS is faster than PMOS.

## Slide 11
Example: dopant compensation
Consider a Si sample doped with 1016/cm3 Boron. What is its electrical resistivity?
Carrier mobility: p=450cm2/Vsec.
Consider the same Si sample (with 1016/cm3 Boron), doped additionally with 1017/cm3 Arsenic. What is the new resistivity?
Carrier mobility: n=600cm2/Vsec. (lower n because higher doping reduces mobility)
The sample is converted to n-type material by adding more donors than acceptors, and is said to be “compensated”.

## Slide 12
Summary of doping terminology

## Slide 13
Chapter 1 Introduction and Historical Perspective
Introduction.
Growth of IC – Moore’s law.
Some history in IC industry.
Semiconductors.
Semiconductor devices, semiconductor technology families.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 14
p - n junction diode
In equilibrium (no bias), drift current (due to ‘built-in’ electric field ) and diffusion current (due to free carrier concentration gradient) exactly balance, so that no net current flows.
For forward bias, the applied field partially cancels the built-in field, allowing majority carriers from both sides to diffuse across the junction.
For reverse bias, the depletion region is widened, only very small leakage current flows.
The overall I-V relation is simply:
(depletion: no free carriers)

## Slide 15
MOS transistor
MOS: metal oxide semiconductor.
MOSFET: MOS field effect transistor.
In accumulation, the channel is rich with holes with little free electrons, and the two PN+ diodes are either zero bias or reverse biased, so there is no/little current between source and drain. The same is true for depletion state where there is no carrier in the channel.
In inversion, the gate voltage is very high which attracts electrons to the very top surface of the channel, so now there is a conduction path of free electrons between source and drain.
depletion region
(holes h+ accumulate to surface)
(electrons e- appeared at surface)
OFF
ON
Intermediate
G: gate
S: source
D: drain

## Slide 16
Bipolar junction transistor (BJT)
The key is that the base is very narrow, so it is totally different from two independent p-n junctions (one forward, one reverse biased) connected through the base region.
In operation, the emitter is grounded, a small positive voltage to base, and a large positive voltage applied to the collector.
A tiny change of VB leads to a large (exponential) change of IE that is very close to collector current IC. (i.e. VB to control IC)
Since most of the current in a BJT flows below the silicon surface, the device is much less sensitive to passivation/protection problems than is the MOS transistor.
For this reason, BJT was used in the earliest ICs in the 1960s while researchers were trying to understand the stability problems of the Si/SiO2 interface for MOS transistor.
Figure 1-31 Simplified cross section (left) and 1D representation (right) of a bipolar transistor. The shaded areas are the depletion regions. The arrows indicate the path of carrier through the device.
Emitter Base Collector

## Slide 17
Semiconductor technology families
1960s, BJT:
BJT: bipolar junction transistor.
Gas phase diffusion for doping.
N- layer grown on P by epitaxy.
Reverse biased p-n junction for device isolation.
6-8 photolithography steps.
1970s, E/D NMOS:
E/D = enhancement/depletion mode
LOCOS (local oxidation) isolation.
NMOS is used since electron mobility is 3 that of hole mobility.
Depletion NMOS took small area, thus denser circuit.
Again, 6-8 photolithography steps.
Left: enhancement (regular) NMOS (device is OFF at zero gate bias).
Right: depletion mode NMOS (device is ON at zero gate bias).
Figure 1-32 Technology typical of the 1960s. Bipolar transistors and resistors were the dominant components.

## Slide 18
Semiconductor technology families
1980s, CMOS:
CMOS: complementary (equal number of NMOS and PMOS) MOS.
Low power consumption, low heating.
E.g. the CMOS inverter consumes no DC current in either state (no DC power).
Higher level integration.
12-14 photolithography steps.
1990s, BiCMOS:
Bipolar and CMOS.
CMOS for highly integrated internal circuit.
BJT for driving circuit.
>20 photolithography steps.
CMOS
BJT
TiSi Un-doped poly p+ poly n+ poly metal
BJT: bipolar junction transistor
poly = poly-crystalline Si.
Figure 1-34 Technology typical of the 1980s. CMOS circuits with both NMOS and PMOS devices were dominant.