## Slide 1
Chapter 2 Modern CMOS technology
Introduction.
CMOS process flow.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
In the simplest CMOS technologies, we need to realize simply NMOS and PMOS transistors for circuits like those illustrated below.
Typical CMOS technologies in manufacturing add additional steps to implement multiple device VTH, thin film transistors (TFT) in SRAMs, capacitors for DRAMs etc.
CMOS described here requires 16 masks (through metal level 2) and >100 process steps.
There are many possible variations on the process flow (e.g. LOCOS device isolation vs. shallow trench isolation).
n-MOS & p-MOS require different channel background doping and source/drain region doping.
In CMOS, the gate is no longer “metal”, it is heavily doped poly-crystalline Si with low resistance.
CMOS: complementary metal–oxide–semiconductor

## Slide 3
CMOS (n-MOS & p-MOS) reduces static power dissipation.
Because (e.g. for the inverter) there is no current flow from +V to GND since one of the MOS is always off.
The same inverter logic can also be realized by replacing the top PMOS with a resistor R (ON NMOS << R << OFF NMOS), but current flows when NMOS is on.
CMOS is required by logic circuits
Inverter:
Output = Input
NOR:
Output = IN1+IN2
Output = GND = 0 if any Input or both are +V = 1
S
D
D
S

## Slide 4
N-MOSFET (field effect transistor) operation
Body (bulk Si) is commonly tied to ground (0V).
When the gate is at a low voltage:
P-type body is at low voltage, source-channel-drain is N+PN+.
If drain is positive bias (i.e. electrons flow from the source and ‘drained’ to the drain), the right side PN+ diode is in reverse bias.
Left side N+P is in zero-bias, as source is usually connected to the grounded bulk Si.
No current flows through the channel, transistor is OFF
When the gate is at a high voltage:
Positive charge on gate of MOS capacitor.
Negative charge attracted to the top surface just below the gate oxide.
Inverts a channel under gate to n-type, source-channel-drain is N+NN+.
Now current can flow through n-type silicon from source through channel to drain, transistor is ON.
Inverted to n-type

## Slide 5
P-MOSFET (field effect transistor) operation
Body tied to high voltage (= source voltage, supply voltage).
Gate low (grounded, which is lower than high voltage bulk Si): transistor is ON.
Gate high (same as bulk Si): transistor is OFF.
Since voltage has only a relative meaning. This is equivalent to the situation of: grounded body/bulk Si, grounded source, negative (< 0V) drain voltage (so holes flow from source and ‘drained’ to drain).
Then transistor is ON when gate is negatively biased, and OFF when gate is grounded.

## Slide 6
Transistors as switches
We can view MOS transistors as electrically controlled switches, and voltage at gate controls path from source to drain.
Notes: Students have hard time to understand this part.

## Slide 7
CMOS inverter
Inverter:
Output = Input
g=Input=0, NMOS is off, PMOS is on. Output=+V=1.
When Input =1, Output=GND=0

## Slide 8
CMOS NAND gate
Output = 0 only when both Inputs are 1

## Slide 9
p
Cross-section of the CMOS IC
This is what we are going to fabricate in this chapter.

## Slide 10
Fabrication “toolkit”
Insulating Layers
  Oxidation, nitridation
  Deposition (LPCVD, PECVD, APCVD)
Selective doping of silicon
  Diffusion (in-situ doping)
  Ion implantation
  Epitaxy (in-situ doping)
Material deposition (silicon, metals, insulators)
  LPCVD
  PECVD
  Sputter deposition
Patterning of Layers
  Lithography (UV, deep UV, e-beam & x-ray)
Etching of (deposited) material
  Dry etches—plasma, RIE, sputter etch, DRIE
  Wet etches—etch in liquids, CMP etc
LPCVD: low pressure chemical vapor deposition.
PECVD: plasma enhanced CVD.
APCVD: atmospheric pressure CVD
RIE: reactive ion etching
DRIE: deep RIE.
CMP: chemical mechanical polishing

## Slide 11
Chapter 2 Modern CMOS technology
Introduction.
CMOS process flow.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 12
Substrate selection: moderately high resistivity (lightly doped, 1015cm-3), (100) orientation substrate (better Si/SiO2 interface than other orientations), P type.
Start from low doping, then dope P-well and N-well by ion implantation that is much better controlled than substrate doping (done during crystal growth).
Wafer cleaning, thermal oxidation (≈ 40 nm, using O2, or H2O generated from H2 and O2 reaction, cleaner than H2O vapor from boiling water), Si3N4 LPCVD (≈ 80 nm), photoresist spinning and baking (≈ 0.5 - 1.0 μm).
Choosing the substrate and active region formation
Nitride has high tensile stress, oxide has compressive stress. The two stress can balance/compensate each other to reduce stress in Si that may cause defects in Si.
LPCVD nitride: 3SiH4+4NH3  Si3N4+12H2, 800oC.
LPCVD: low pressure chemical vapor deposition

## Slide 13
Mask #1 patterns the active areas. The nitride is dry etched.
Dry etch = plasma etch, reactive species are generated in a plasma (like arc discharge). E.g F is generated in CF4 plasma. Atomic F is extremely reactive.
Si3N4 + 12F  3SiF4 (gas/volatile, pumped away) + 2N2
Active region formation
Photolithography, nitride etching

## Slide 14
LOCOS isolation
Remove photoresist.
Field oxide is grown using a LOCOS process.
Typically 90min @ 1000˚C in H2O grows SiO2 ≈ 0.5 µm.
LOCOS: LOCal Oxidation of Silicon
http://en.wikipedia.org/wiki/LOCOS
Remove resist, thermal oxidation
Field oxide is partially recessed into the surface (oxidation consume some of the silicon)
Field oxides forms a lateral extension under the nitride layer – bird’s beak region
Bird’s beak region limits device scaling and device density in VLSI circuits!
Si3N4 is very dense material and prevents/blocks H2O or O2 from diffusion to the Si surface, thus no oxidation under nitride.

## Slide 15
Alternative process to LOCOS isolation:
shallow trench isolation with filled implants (here P+)
Growth of pad silicon dioxide and deposition of silicon nitride as in LOCOS
Implant trench to increase field threshold (for better device isolation) and growth of liner oxide for passivation and smoothing
Trench fill with deposited oxide (not thermally grown oxide)
CMP (chemical mechanical polishing) for planarization.
LOCOS:
Bird’s Beak problem, unsuitable for small device.
Note: this process added P+ impanation, slightly different from the process in textbook.

## Slide 16
P-well formation
Mask #2 blocks a B+ implant to form the wells for the NMOS devices. Typically dose 1013cm-2 @ 150-200 KeV (very high energy).
(Implant dose is in cm-2, doping concentration is in cm-3)
Wet etch away Si3N4, spin photoresist, lithography, B+ implantation.
In ion implantation, positive B+ ions are formed by exposing the source gas containing B to an arc discharge.
Only B + is selected by a bending magnet to pass through a slit.
B + energy is high enough to pass through the field (LOCOS) oxide. But photoresist is thick enough to block the ions.

## Slide 17
N-well formation
Strip photoresist, spin resist and photolithography, ion implantation
Mask #3 blocks a P+ implant to form the wells for the PMOS devices.
Typically 1013 cm-2 @ 300-400 KeV.
(P is heavier than B, so higher energy needed)

## Slide 18
N- and P- well formation
Remove resist and anneal
A high temperature drive-in produces the “final” well depths and repairs implant damage.
Typically 4-6 hours @ 1000˚C - 1100˚C or equivalent Dt.
(here D is diffusion coefficient, t is time)
Ion energy is 100keV, much higher than energy needed to break 4 Si bonds (total 12eV), so ion implantation induces many damages.
B and P have similar diffusion coefficient, so similar final well depth.

## Slide 19
Threshold voltage (VTH) adjustment
Mask #4 is used to mask the PMOS devices.
A VTH adjust implant is done on the NMOS devices.
Typically 1-5 x 1012cm-2 B+ implant @ 50 - 75 KeV.
Spin photoresist, photolithography, B+ ion implantation
Note: section 2.2.5 is skipped
Implant dose
Figure 2-22

## Slide 20
Threshold voltage (VTH) adjustment
Remove resist, then spin photoresist, photolithography, As+ ion implantation
Mask #5 is used to mask the NMOS devices.
A VTH adjust implant is done on the PMOS devices.
Typically 1-5 x 1012 cm-2 As+ implant @ 75 - 100 KeV.
Again, adjust VTH by controlling implant dose QI.