## Slide 1
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Single crystal silicon
Three types of solids - amorphous, polycrystalline, mono-crystalline (single-crystal).
Semiconductor devices and VLSI (very large scale integrated) circuits require high-purity single-crystal semiconductors. Because:
  Difficult to control properties of amorphous or poly-crystals.
  By doping, electronic properties (carrier density, mobility, conductivity, carrier lifetime) of a single crystal can be controlled more precisely.
Amorphous silicon is used in photovoltaic cells, electronic displays (large-area).
Polycrystalline silicon is used as a gate contact in MOSFETs (VLSI circuits).
Single crystal Si wafers
Diameters: currently up to 300mm (500mm?)
Wafer thickness: 650μm
Wafer purity: 150 parts/trillion
Impurities: 99.99999999% Si

## Slide 3
Microstructure of electronic materials
SiO2
gate oxide
Polycrystalline materials

## Slide 4
Crystals are characterized by a unit cell which repeats in the x, y, z directions.
Crystallography - introduction
Planes and directions are defined using an x, y, z coordinate system.
[111] direction is defined by a vector having components of 1 unit in x, y and z.
Planes are defined by Miller indices - reciprocals of the intercepts of the plane with the x, y and z axes.
For the (110) plane, it has intercepts with x, y, z-axis of 1, 1,  (i.e. no intercept with z-axis). So its Miller indices are (1/1, 1/1, 1/)=(1,1,0).
For any plane (l, m, n), it is always perpendicular to the direction [l, m, n].
E.g. [111] direction is perpendicular to (111) plane.

## Slide 5
Diamond Structure of Si
Silicon has the basic diamond crystal structure:
Two merged FCC cells offset by a/4 in x, y and z.
http://jas.eng.buffalo.edu/education/solid/unitCell/home.html
This website has a 3D structure at various viewing angles.

## Slide 6
Point defects: vacancy, interstitial, substitutional, Frankel defects
Linear defects: edge and screw dislocations
Planar defects: stacking fault, grain boundaries, surfaces
Bulk defects: cracks and pores, precipitate
Defect in crystals

## Slide 7
Point defects
Point defects.
Substitutional.
Interstitial.
Vacancy (Schottky defect).
Frenkel-type defect (interstitial - vacancy pair).
Point defects dictate most dopant diffusion mechanisms, and thus determine the impurity profile.

## Slide 8
The number of neutral vacancies is thermodynamically determined by,
where No is the density of atoms/cm3 and Ea is the activation energy for the formation of the vacancy (in silicon, No=5.021022/cm3 and Ea=2.6 eV)
Point defects: vacancies and substitutional
Substitutional can be foreign unwanted impurities, or intentionally introduced impurities.
You may want a dopant impurity to be on a substitutional site, but you may not want a heavy metal atom or other unwanted impurity to be on a substitutional site (harder to remove).

## Slide 9
Interstitials can be foreign unwanted impurities, intentionally introduced impurities, or “misplaced” host atoms (an intrinsic defect, the self-interstitial).
Dopant atoms diffuse through the semiconductor faster as interstitials, but we need to place them in substitutional sites to make use of them (i.e. they act as dopants only when in substitutional sites).
Point defects: interstitial
Energies involved for the atomic diffusion of interstitial impurities

## Slide 10
A missing line or additional line of atoms is called a dislocation.
Dislocations are either pure edge, pure screw or a combination of both types.
Line defects: dislocation
Screw dislocations give a helical structure to the planes, often show up in crystal growth

## Slide 11
Dislocation affects deformation properties - to slide upper block over lower now only requires a line of bonds to break at a time, not a whole plane process of slip.
It causes low yield strength of solids.
Dislocation sources: by stress due to temperature gradient, due to agglomeration.
Dislocation move

## Slide 12
A stacking fault is a disruption in the stacking of layers in the crystal.
It is terminated by dislocation.
Planar defects: stacking faults
Volume defects: precipitates
Precipitates are three dimensional defects that have a different chemical makeup from the host lattice.
They can result from an impurity exceeding the maximum solubility of the crystal (much like super-saturation of sugar in water).

## Slide 13
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers

## Slide 14
Raw material preparation

## Slide 15
Economical value

## Slide 16
Quartzite (sand, SiO2) is placed in a hot (1800oC) furnace with carbon releasing materials, and reacts as shown, forming metallurgic grade silicon (MGS):
2SiO2(solid) + 2C(solid)  Si(liquid) + 2CO(gas)
Metallurgical grade silicon
Metallurgical grade silicon (~98% pure) production and typical impurity levels.
Over 50% MGS is used to make Al alloys.
The fraction used for semiconductors is very small.

## Slide 17
Electrical grade silicon (polycrystalline)
Basically, the solid Si is first converted into a liquid form (SiHCl3) for purification, then converted back into solid Si.
Both reactions occur at high temperatures.
Metallurgical grade silicon is treated with hydrogen chloride to form trichlorosilane:
Si + 3HCl  SiHCl3(g) + H2(g) (use catalyst)
SiHCl3 is liquid at room temperature, boiling point 32oC. Multiple distillation of the liquid removes the unwanted impurities (99.9999% pure).
The purified SiHCl3 is then used in a hydrogen reduction reaction to prepare the electronic grade Si (EGS):
SiHCl3(g) + H2(g)  Si(s) + 3HCl(g)
(this is the reverse reaction of the above reaction)
EGS is the raw material for Si single crystal production.

## Slide 18
Jan Czochralski (cho-HRAL-skee) (1885 - 1953) was a Polish chemist who invented the Czochralski process, which is used to grow single crystals and is used in the production of semiconductor wafers.
He discovered the Czochralski method in 1916 when he accidentally dipped his pen into a crucible of molten tin rather than his inkwell. He immediately pulled his pen out to discover that a thin thread of solidified metal was hanging from the nib. The nib was replaced by a capillary, and Czochralski verified that the crystallized metal was a single crystal.
Si single crystal growth
Two methods used: Czochralski (CZ) and float zone (FZ).
http://en.wikipedia.org/wiki/Jan_Czochralski

## Slide 19
Czochralski method (CZ)
It is widely employed for Si, GaAs, and InP.
The EGS is broken into small pieces and placed in an SiO2 crucible.
In an argon ambient, the crucible is heated to just above 1417oC.
Dopant is added to the melt to intentionally dope the resulting crystal.
A single crystal seed is then lowered into the melt (crystal orientation and wafer diameter determined by seed orientation and pull rate), and withdrawn slowly.
Melt flows up the seed and cools as crystal begins to grow.
Seed rotated about its axis to produce a circular cross-section crystal. The rotation inhibits the natural tendency of the crystal to grow along certain orientations to produce a faceted crystal.
Long ingots (boules) 100 kg, with very good circular cross-section are produced.
The oxygen and carbon (from graphite furnace components), contribute about 1017-1018/cm3 contaminants.

## Slide 20
Czochralski method (CZ)

## Slide 21
A commercial CZ puller Early in the growth process Later in the growth process
Czochralski growth of silicon

## Slide 22
Oxygen and carbon in CZ silicon
The CZ growth process inherently introduces O (from SiO2 crucible) and C (from graphite susceptor/supporter).
Typically, CO ≈ 1018 cm-3 and CC ≈ 1016 cm-3.
The O in CZ silicon often forms small SiO2 precipitates in the Si crystal under normal processing conditions.
O and these precipitates can actually be very useful: provide mechanical strength, internal gettering.
Figure 3-25 Point defect and diffusion mechanisms that contribute to the growth or shrinkage of SiO2 precipitates in silicon.
Critical size is about 1nm: stable precipitates above 1nm, may shrink and disappear below 1nm.