## Slide 1
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
(1)
Czochralski process - crystal growth rate
Freezing occurs between isotherms X1 and X2.
latent heat of fusion (i.e. crystalization) + heat conducted from melt to crystal
(A)
heat radiated away
(C).
heat conducted through the crystal
(B)
=
=
(A)
(B)
We wish to find a relationship between pull rate and crystal diameter.
Heat balance:
A1,2 = Cross-sectional area

## Slide 3
The rate of growth of the crystal is
where vP is the pull rate and N is the density.
Neglecting the middle term in Eqn. (1) we have:
(2)
(3)
In order to replace dT/dx2, we need to consider the heat transfer processes.
Heat radiation from the crystal (C)
is given by the Stefan-Boltzmann law*:
Heat conduction up the crystal is
given by
(4)
(5)
Czochralski process - crystal growth rate
2πrdx = radiation surface.
σ = Boltzman constant (NOT kB)
kS = thermal conductivity of the solid.
=1 for perfect blackbody.
<1 for “grey-body”.
*Stephen-Boltzmann law: http://en.wikipedia.org/wiki/Stefan%E2%80%93Boltzmann_law

## Slide 4
• Differentiating (5), we have
(6)
• Substituting (6) into (4), we have
(7)
• kS varies roughly as 1/T, so if kM is the
thermal conductivity at the melting point,
(8)
(9)
• Solving this differential equation, evaluating it at x = 0 and substituting the
result into (3), we obtain (see text):
(10)
Czochralski process - crystal growth rate
Vpmax = maximum pull rate, inversely proportional to the square root of crystal radius.

## Slide 5
Crystal growth rate: example
4 hours to pull one meter long boule.
However, this equation is not so accurate, and in practice feedback is used to adjust the pulling rate in order to maintain constant diameter.
For perfect blackbody: =1
For “grey” body: <1

## Slide 6
Dopant incorporation during crystal growth
Dopants are added to the melt to provide a controlled N or P doping level in the wafers.
However, the dopant incorporation process is complicated by dopant segregation.
Generally, impurities “prefer to stay in the liquid” as opposed to being incorporated into the solid.
This process is known as segregation. The degree of segregation is characterized by the segregation coefficient, ko, for the impurity.
CS
CL
CS and CL are the impurity concentration just on the either side of the solid/liquid interface.

## Slide 7
Most k0 values are <1 which means the impurity prefers to stay in the liquid.
Thus as the crystal is pulled, dopant concentration will increase.
In other words, the distribution of dopant along the ingot will be graded.
Dopant behavior during crystal growth

## Slide 8
Distribution coefficient: example
=1.019×10-4mol

## Slide 9
Dopant incorporation during crystal growth
VO = initial volume
IO = number of impurities
CL = impurity concentration in the melt
C0 = initial impurity concentration in the melt C0 = I0/V0
By definition: CS/CL=k0
If during growth, an additional volume dV freezes, the impurities incorporated into dV are given by:
The impurity level in the crystal (Cs)
f = Vs/Vo, the ratio of solid silicon to the initial liquid volume.

## Slide 10
Doping concentration versus position along the grown CZ crystal for common dopants in silicon
Note the relatively flat profile produced by boron with a ko close to 1.
Dopants with ko << 1 produce much more doping variation along the crystal.
Doping concentration in a solid as a function of the fraction solidified.
(but no dopant has ko>1)

## Slide 11
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers

## Slide 12
For CZ-grown Si, impurities (O and C) can be introduced from the melt contacting the SiO2 crucible and from graphite susceptor/supporter.
This limits the resistivity to 20Ωcm, while intrinsic Si is 230kΩcm.
These crystals are more expensive and have very low oxygen and carbon and thus, are not suitable for the majority of silicon IC technology.
Carrier concentrations down to 1011 atoms/cm3 have been achieved.
It is far less common, and is reserved for situations where oxygen and carbon impurities cannot be tolerated.
Float-zone does not allow as large Si wafers as CZ does (200mm and 300mm) and radial distribution of dopant in FZ wafer is not as uniform as in CZ wafer.
It is good for solar cells, power electronic devices (thyristors and rectifiers) that use the entire volume of the wafer not just a thin surface layer, etc.
Float-zone crystal growth: overview

## Slide 13
Float-zone crystal growth process
Polycrystalline silicon is converted into single-crystal by zone heating (zone melting).
The entire poly-Si rod from the EGS process is extracted as a whole.
The rod is clamped at each end, with one end in contact with a single crystal seed.
An RF heating coil induces eddy currents (power I2R) in the silicon, heating it beyond its melting point in the vicinity of the coil.
The "floating" melt zone is about 2cm wide/high.
The seed crystal touches the melt zone and is pulled away, along with a solidifying Si boule following the seed. The crystalline direction follows that of the seed single crystal.
Limited to about a 4" wafer, as the melt zone will collapse - it is only held together by surface tension (and RF field levitation).
Poly-Si
c-Si
RF coil
Melt is not held in a container, it is “float”, thus the name “float zone”.

## Slide 14
Float-zone: zone refining
Dopants/impurities prefer to stay in the liquid than in the solid.
Thus, the impurities generally stay in the melt zone, and don't solidify in the boule.
That is, segregation (and evaporation) of impurities in the melt zone help purify the Si further.
One can "purify" FZ wafers further by successively passing the coil along the boule. The impurities then segregate towards the end of the boule.
Of course, if neglecting impurity evaporation, the total amount of impurity is the same. Yet the impurity at the lower part is much lower than, and at the upper part approaches to, the original impurity concentration.
Thermal instability in the melt zone can cause micro-variations in composition and doping. Difficult in making a uniform dopant concentration.

## Slide 15
Doping in FZ growth
(Doping can of course be achieved if the starting material poly-crystalline Si rod is doped. But due to zone-refining, the doping is not uniform along the boule)
Gas doping:
Dopants are introduced in gaseous form during FZ growth.
n-doping: PH3 (Phosphine), AsCl3
p-doping: B2H6 (Diborane), BCl3
Good uniformity along the length of the boule.
Pill doping:
Drill a small hole in the top of the EGS rod, and insert the dopant.
If the dopant has a small segregation coefficient, most of it will be carried with the melt as it passes the length of the boule.
Resulting in only a small non-uniformity.
Ga and In doping work well this way.

## Slide 16
Zone refining
Zone length is L. The rod has initial uniform impurity concentration of C0.
If the molten zone moves upwards by dx, the number of impurities in the liquid (=I) will change since some will be dissolved into the melting liquid at the top (=C0dx) and some will be lost to the freezing solid on the bottom (=CSdx=k0CLdx). Thus: (assume cross-sectional area =1)

## Slide 17
Floating zone crystal growth – zone refining
Impurity during float-zone growth or zone refining. One pass of the molten zone through the solid.
L is the length of the molten zone (2cm)
Zone refining with multiple passes, k0=0.1. L is the length of the molten zone.

## Slide 18
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers

## Slide 19
Steps for wafer preparation

## Slide 20
Ingot grinding

## Slide 21
Traditional method of slicing Wire saw for large wafers
Wafer slicing
The saw blade itself is about 400m thick, together with the loss at the seed and tail end of the crystal, only 50% of the boule ends up in wafer form.
After slicing, mechanical lapping and wet chemical etching is performed before final chemical mechanical polishing. The wet etching is typically:
3Si + 4HNO3 + 18HF  3H2SiF6 + 4NO + 8H2O

## Slide 22
Wafer polishing
Chemical mechanical polishing
The rotation and pressure generates heat that drives a chemical reaction in which OH- radicals from the NaOH oxidize the silicon. The SiO2 particles abrade the oxide away.
Slurry consists of nano-particles (10nm SiO2 or Al2O3) and chemicals (NaOH).

## Slide 23
Common (not always) wafer surface orientation
{100} wafer usually breaks along {110} plane (actually Si cleaves naturally along {111} plane, which meet the surface at an angle of 54.7o, the angle between <001> and <111>).
Sometimes (not often) {100} wafers break along {100} plane. ({100} = (100)+(010)+(001))
Another flat configuration for {100} n-type wafer
Should be {110} plane

## Slide 24
Advantage of larger diameter wafers
More chips per wafer for larger wafer.

## Slide 25
Silicon crystal structure and defects.
Czochralski single crystal growth.
Growth rate and dopant incorporation for CZ method.
Float zone single crystal growth and doping.
Wafer fabrication.
Measurement methods.
Chapter 3 Crystal growth, wafer fabrication and basic properties of silicon wafers

## Slide 26
Hot probe measurement of carrier type
The hot probe technique is used to determine the type of dopant in a wafer.
It relies on the generation of the Seebeck voltage (open circuit), i.e. the diffusion of free carriers (electrons or holes) as a result of a temperature gradient.
The sign of the voltage tells the carrier type.
Alternatively, one can measure the current direction (short circuit).
The current that flows due to the majority carrier is given by
Pn is thermoelectric power, negative for electrons, positive for holes.
Vm
Hot
Cold
e-
n-type wafer

## Slide 27
Electrical measurement techniques – four point probe
The four point probe method measures the resistance/resistivity of a wafer.
Using values of carrier mobility, one can calculates the carrier concentration.
Use four points (rather than two) to eliminate the effect of contact resistance.
V
I
S
t
d
=(en)-1,  is mobility, n is carrier density.

## Slide 28
Silicon is placed inside a magnetic field and the resultant motion of charge will experience a force perpendicular to the electric field. F=qvB
In equilibrium this results in a transverse potential difference known as the Hall voltage VH. (such that F=qE=qVH/w=qvB, i.e. forces are balanced, so VH=vBw)
The magnitude and sign of the Hall voltage leads directly to the carrier concentration, type, and mobility (if the resistivity is known).
Current density j=I/tw=E/=qnv, VH=vBw=(I/twqn)Bw=IB/tqn.
Hall coefficient RH  VHt/BI=1/qn=μH, μH is Hall mobility (we know that =1/qn).
(μH is slightly lower than conductivity mobility, due to more scattering when magnetic field is present.  can be measured from four-point probe)
Hall measurement of carrier type & mobility
Thickness of the slab is t (along B direction), width is w (along VH direction). VH is measured, and used to calculate RH. Then carrier concentration p, n=1/qRH.
Hall voltage (VH) measurement

## Slide 29
GaAs Liquid Encapsulated CZ (LEC):
GaAs single crystal is more difficult to grow than Si.
At 1238oC, the vapor pressure of As is 10 atmospheres, while Ga is only 0.001 atmospheres.
So As is rapidly lost to evaporation, resulting in Ga-rich melt (non-stoichiometric).
A cap is used to encapsulate the melt and stop evaporation.
This cap is typically B2O3 that melts at 400oC.
This allows the seed crystal to be lowered through the liquid cap and pulled out of the cap.
Crystal CZ growth: GaAs

## Slide 30
Horizontal Bridgman GaAs growth
Historically, high defect density with LEC GaAs limits its use from electronic applications.
Most GaAs for optoelectronics is produced by Bridgman method.
The GaAs charge is held in a sealed ampoule with excess arsenic.
Thus, higher As pressure can be reached that limits As evaporation.