## Slide 1
Chapter 4 Clean room, wafer cleaning and gettering
Introduction.
Clean room.
Wafer cleaning.
Gettering.
Measurement methods.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Effect of defect and contamination on semiconductor industry
Importance of unwanted impurities increases with shrinking geometries of devices.
75% of the yield loss is due to defects caused by particles (1/2 of the min feature size).
LLS: localized light scatters (use laser to detect and count particles)
GOI: gate oxide integrity, by electrical measurement
Requirement different for DRAM and logic chip, due to greater gate insulator area on DRAM chip.
109/cm2  0.0001% monolayer

## Slide 3
Contaminants may consist of particles, organic films, photoresist, heavy metals or alkali ions.
Modern IC factories employ a three tiered approach to controlling unwanted impurities:
clean factories
wafer cleaning
gettering
Type of contaminants

## Slide 4
Effects on MOSFET: two examples
MOSFET threshold voltage is given by:
If tox=10nm, then a 0.1V Vth shift can be caused by Na+ or K+ of QM=2.151011 ions /cm2 (<0.1% monolayer or 10ppm in the oxide).
0=8.8510-12F/m, ox=3.9
For MOS DRAM, refresh time of several msec requires a generation lifetime of
This requires trap density Nt1012/cm3, or 0.02ppb (1012/(51022)=0.02ppb).
( is trap capture cross-section, vth is minority carrier thermal velocity; Vth107cm/sec, 10-15cm-2)
Deep-level traps (Cu, Fe, Au etc.) pile up at the surface where the devices are located. This causes leak current. Need refresh/recharge the MOS capacitor.
DRAM: Dynamic Random Access Memory

## Slide 5
Residual contaminants affect kinetics of processes, here oxidation.
Effects of cleaning on thermal oxidation

## Slide 6
Particle contaminants
Particle sources: air, people, equipment and chemicals.
A typical person emits 5-10 million particles per minute.
 | >0.2m | >0.5m
NH4OH | 130-240 | 15-30
H2O2 | 20-100 | 5-20
HF | 0-1 | 0
HCl | 2-7 | 1-2
H2SO4 | 180-1150 | 10-80
Particle density (number/ml) for ULSI grade chemicals
ULSI: ultra-large-scale integration

## Slide 7
Fe, Cu, Ni, Cr, W, Ti…
Na, K, Li…
Metal contamination
Sources: chemicals, ion implantation, reactive ion etching, resist removal, oxidation.
Effects: defects at interface degrade device; leads to leak current of p-n junction, reduces minority carrier life time.
Dry etching
Ion implantation
Photoresist removal
Wet oxidation
9
10
11
12
13
Log (concentration/cm2)
Fe Ni Cu

## Slide 8
Chapter 4 Clean room, wafer cleaning and gettering
Introduction.
Clean room.
Wafer cleaning.
Gettering.
Measurement methods.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 9
Modern IC factories employ a three tiered approach to controlling unwanted impurities:
clean factories
wafer cleaning
gettering
Clean factory is the first approach against contamination
Clean factory Wafer cleaning Gettering

## Slide 10
Factory environment is cleaned by:
  HEPA filters and recirculation for the air.
  “Bunny suits” for workers.
  Filtration of chemicals and gases.
  Manufacturing protocols.
Clean room
HEPA: High Efficiency Particulate Air
HEPA filters composed of thin porous sheets of ultrafine glass fibers (<1m diameter).
It is 99.97% efficient at removing particles from air.
Room air forced through the filter at 50cm/sec.
Large particles trapped, small ones stick to the fibers due to electrostatic forces.
The exit air is typically better than class 1.

## Slide 11
Class of a clean room
Air quality is measured by the “class” of the facility.
Class 1-100,000 mean number of particles, greater than 0.5m, in a cubit foot of air.
A typical office building is about class 100,000.
The particle size that is of most concern is 10nm – 10m. Particles <10nm tend to coagulate into large ones; those >10m are heavy and precipitate quickly.
Particles deposit on surfaces by Brownian motion (most important for those <0.5m) and gravitational sedimentation (for larger ones).
Class | 0.1 | 0.3 | 0.5 | 5.0
1 | 35 | 3 | 1 | 
10 | 350 | 30 | 10 | 
100 |  | 300 | 100 | 
1000 |  |  | 1000 | 7
10000 |  |  | 10000 | 70
100000 |  |  | 100000 | 700
Particle diameter (m)
by definition

## Slide 12
Particle contamination and yield
Generally, particles on the order of the technology minimum features size or larger will cause defect.
75 yield loss in modern VLSI fabrication facilities is due to particle contamination.
Yield models depend on information about the description of particles.
Particles on the order of 0.1-0.3m are the most troublesome: larger particles precipitate easily; smaller one coagulate into larger particles.

## Slide 13
Chapter 4 Clean room, wafer cleaning and gettering
Introduction.
Clean room.
Wafer cleaning.
Gettering.
Measurement methods.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 14
Cleaning involves removing particles, organics and metals from wafer surfaces.
Particles are largely removed by ultrasonic agitation during cleaning.
Organics (photoresist) are removed in O2 plasma or in H2SO4/H2O2 (Piranha) solutions.
The “RCA clean” is used to remove metals and any remaining organics.
Modern wafer cleaning
Typical person emit 5-10 million particle per minute.
Most modern IC plants use robots for wafer handling.
A cassette of wafers

## Slide 15
RCA clean is “standard process” used to remove organics, heavy metals and alkali ions.
Ultrasonic agitation is used to dislodge particles.
SC: Standard Cleaning
RCA: Radio Corporation of America, now makes TV, stereos…
Standard RCA cleaning procedure
DI water: de-ionized water
and all contaminants on top of it, but induces H passivated surface (bad)
Less NH4OH will reduce surface roughness
not removed by SC-1
HF dip added to remove oxide

## Slide 16
SC-1:
NH4OH(28%):H2O2(30%):H2O=1:1:5 - 1:2:7; 70-80C, 10min, high pH.
Oxidize organic contamination (form CO2, H2O…)
Form complex such as Cu(NH3)4+2 with metals (IB, IIB, Au, Ag, Cu, Ni, Zn, Cd, Co, Cr).
Slowly dissolve native oxide and grow back new oxide, which removes particles on oxide.
But NH4OH etches Si and make the surface rough, thus less NH4OH is used today.
Standard cleaning (SC)
SC-2:
HCl(73%):H2O2(30%):H2O=1:1:6 - 1:2:8; 70 - 80C; 10min, low pH.
Remove alkali ions and cations like Al+3, Fe+3 and Mg+2 that form NH4OH insoluble hydroxides in basic solutions like SC-1.
These metals precipitate onto wafer surface in the SC-1 solution, while they form soluble complexes in SC-2 solution.
SC-2 also complete the removal of metallic contaminates such as Au that may not have been completely removed by SC-1 step.

## Slide 17
(1)
(2)
Principles of metal cleaning
If we have a water solution with a Si wafer and metal atoms and ions, two reactions take place.
The two reactions will proceed in opposite directions, one providing electrons, which will then be consumed by the other (forming an oxidation/reduction couple). In this couple, the stronger reaction will dominate.
Generally, (2) is driven to the left and (1) to the right so that SiO2 is formed and M plates out on the wafer.
Good cleaning solutions drive (2) to the right since M+ is soluble and will be desorbed from the wafer surface.

## Slide 18
Reaction goes to the left
The strongest oxidants are at the bottom (H2O2 and O3). These reactions go to the left, grabbing electrons and forcing (2) in previous slide to the right.
Fundamentally the RCA clean works by using H2O2 as a strong oxidant.
Principles of metal cleaning

## Slide 19
H2O  H++OH- [H+]=[OH-] = 6x10-13cm-3
Diffusivity of: H+ ≈ 9.3x10-5cm2s-1  µH+=qD/kT=3.59cm2V-1s-1
of : OH- ≈ 5.3x10-5cm2s-1  µOH-=qD/kT=2.04cm2V-1s-1
Ultrasonic cleaning and DI water
RCA cleaning with ultrasonic agitation is more effective in removing particles.
Ultrasonic cleaning:
Highly effective for removing surface contaminants
Mechanical agitation of cleaning fluid by high-frequency vibrations (between 20 and 45 kHz) to cause cavitation - formation of low pressure vapor bubbles that scrub the surface.
Higher frequencies (>45kHz) form smaller bubbles, thus less effective.
However, megasonic (1MHz) cleaning is also found effective in particle removal.
DI (de-ionized) water is used for wafer cleaning.
One monitors DI water by measuring its resistivity, which should be >18Mcm.
Einstein relation: µ=qD/kT, http://en.wikipedia.org/wiki/Einstein_relation_%28kinetic_theory%29

## Slide 20
Other cleaning methods
Dry (vapor phase) cleaning:
Energy may come from plasma, ion beam, short-wavelength (UV) radiation or heating.
HF/H2O vapor cleaning
UV-ozone cleaning (UVOC)
H2/Ar plasma cleaning
Thermal cleaning
Ohmi cleaning: room temperature, fewer chemicals

## Slide 21
Chapter 4 Clean room, wafer cleaning and gettering
Introduction.
Clean room.
Wafer cleaning.
Gettering.
Measurement methods.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 22
Gettering
For the alkali ions, gettering generally uses dielectric layers on the topside; PSG for trapping, or Si3N4 layer for blocking them from getting into the device region.
PSG: phosphosilicate glass, is a P2O5/SiO2 glass that is normally deposited by CVD, usually contains 5% by weight phosphorus.
PSG traps alkali ions (Na+, K+) and form stable compounds.
At higher than room temperature, alkali ions can diffuse into PSG from device region and trapped there.
Problems with PSG: it affects electric fields since dipoles exist in PSG, and it absorb water, leading to Al corrosion.
For metal ions, gettering generally uses traps on the wafer backside or in the wafer bulk. Here gettering works because the metals (Au…) do not “fit” in the silicon lattice easily because of their very different atomic size, thus they prefer to stay at defect sites.
Therefore, the idea of gettering is to create such defect sites outside of active device region.
Backside = external gettering: roughing/damaging the backside of the wafer, or depositing a poly-silicon layer, to provide a low energy “sink” for impurities.
Bulk = intrinsic (or internal) gettering: using internal defects to trap impurities, thus moving them away from the active region of the wafer.

## Slide 23
Deep level impurities in silicon:
large diffusivity, easily trapped by mechanical defects or chemical traps.
Gettering
Figure 4-6 Periodic table indicating the elements that are of most concern in gettering.

## Slide 24
Fast diffusion of various impurities
Heavy metal gettering relies on metal’s very high diffusivity (when in interstitial sites) in silicon, and its preference to segregate to “trap” sites.
Diffusivity (cm2/sec)
Those metal diffuses fast because they do so as interstitials.
Whereas dopants are substitutional and diffuse by interacting with point defects.
I: interstitial
S: substitutional
They can diffuse from front-side to backside of the wafer (>0.5mm distance)

## Slide 25
PSG layer
Devices in near surface region
Denuded zone or epitaxy layer
Intrinsic gettering region
Backside gettering region
500+m 10-20m
Gettering mechanism

## Slide 26
Gettering consists of:
    Making metal atoms mobile.
    Migration of these atoms to trapping sites.
    Trapping of atoms.
Step 1 generally happens by kicking out the substitutional (s) atom into an interstitial (i) site. One possible reaction is: (I = interstitial Si)
Step 2 usually happens easily once the metal is interstitial since most metals diffuse rapidly in this form.
Step 3 happens because heavy metals segregate preferentially to damaged regions (dislocation or stacking fault) or to N+ regions, or pair with effective getters like P (AuP).
Step 1 can be facilitated by introducing large amount of Si interstitials, by such as high density phosphorus diffusion, ion implantation damage or SiO2 precipitation.
Gettering mechanism

## Slide 27
Intrinsic gettering
Oxygen diffusivity:
D0 >> Ddopants but D0<< Dmetals
1100
900
700
500
Out-diffusion of O
Nucleation of SiO2
Precipitation
(growth of SiO2)
denuded zone = oxygen free; thickness several tens of µm
50-100nm in size
Slow ramp
1-3 nm min size of nuclei, concentrations ≈ 1011cm-3
Temperature oC
Time
In intrinsic gettering, the metal atoms segregate to dislocations (formed because of volume mismatch of SiO2 and host Si lattice) around SiO2 precipitates.
15 to 20 ppm oxygen wafers are required:
<10 ppm - precipitate density is too sparse to be an effective getterer.
>20 ppm - wafers tend to warp during the high temperature process.
Note: devices that use the entire wafer as the active region (solar cells, thyristors, power diodes, etc...) can not use this technique, but can use extrinsic gettering.
Today, most wafer manufactures perform this intrinsic gettering task that is better controlled.
Precipitates (size) grow @ high T
Density of nucleation sites grow @ low T
Therefore, low T to increase density, and high T to grow its size.

## Slide 28
Intrinsic Gettering: SiO2 precipitates
no SiO2
SiO2 precipitates (50-100nm)
SiO2 precipitates (white dots) in bulk Si
No SiO2 on top surface
(denuded zone)
Figure 4-13

## Slide 29
Chapter 4 Clean room, wafer cleaning and gettering
Introduction.
Clean room.
Wafer cleaning.
Gettering.
Measurement methods.
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 30
Un-patterned wafers (blank)
  Count particles in microscope
  Laser scanning systems that give maps of particles down to ≈ 0.2 µm
Patterned wafers
  Optical system compares a die with a “known good reference” die (adjacent die, chip design - its appearance)
  Image processing identifies defects
  Test structure (not in high volume manufacturing)
Particle contamination detection
Test structures design to detect defects

## Slide 31
Monitoring the wafer cleaning efficiency
Concentrations of impurities determined by surface analysis.
Excite  Identify (unique atomic signature)  Count concentrations
Primary beam electron good lateral resolution (e can be focused, but not x-ray)
Detected beam electron good depth resolution and surface sensitivity
X-ray poor depth resolution and poor surface sensitivity
ions (SIMS) excellent
ions (RBS) good depth resolution, reasonable sensitivity (0.1 atomic%)
works with SEM
He+ 1-3 MeV
O+ or Cs+ sputtering and mass analyses
emitted