## Slide 1
Introduction and application.
Light source and photomask, alignment.
Photolithography systems.
Resolution, depth of focus, modulation transfer function.
Other lithography issues: none-flat wafer, standing wave...
Photoresist.
Resist sensitivity, contrast and gray-scale photolithography.
Step-by-step process of photolithography.
Chapter 5 Lithography
Note: this chapter covers more topics and details than the textbook. But resolution enhancement techniques (phase-shift mask, off-axis illumination…) and advanced lithographies (electron beam lithography…) will not be covered – they will be covered in NE 353 Nanoprobing and lithography.
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Lithography stone and mirror-image print of a map of Munich.
History
Historically, lithography is a type of printing technology that is based on the chemical repellence of oil and water.
Photo-litho-graphy: latin: light-stone-writing.
In 1826, Joseph Nicephore Niepce in Chalon France takes the first photograph using bitumen of Judea on a pewter plate, developed using oil of lavender and mineral spirits.
In 1935 Louis Minsk of Eastman Kodak developed the first negative photoresist.
In 1940 Otto Suess developed the first positive photoresist.
In 1954, Louis Plambeck, Jr., of Du Pont, develops the Dycryl polymeric letterpress plate.
Lithography press for printing maps in Munich

## Slide 3
Lithography is a printing process that uses chemical processes to create an image.
For instance, the positive part of an image would be a hydrophobic chemical, while the negative image would be water.
Thus, when the plate is introduced to a compatible ink and water mixture, the ink will adhere to the positive image and the water will clean the negative image.
Lithography for art: the print principle

## Slide 4
Photolithography for IC manufacturing
Patterning process consists of:
Mask design
Mask fabrication
Wafer exposure
In IC manufacturing, lithography is the single most important technology.
35% of wafer manufacturing costs comes from lithography.
The SIA roadmap is driven by the desire to continue scaling device feature sizes.
0.7 linear dimension shrink every 3 yr.
Placement/alignment accuracy 1/3 of feature size.
Figure 5.1
Figure 5.2

## Slide 5
Introduction and application.
Light source and photomask, alignment.
Photolithography systems.
Resolution, depth of focus, modulation transfer function.
Other lithography issues: none-flat wafer, standing wave...
Photoresist.
Resist sensitivity, contrast and gray-scale photolithography.
Step-by-step process of photolithography.
Chapter 5 Lithography
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 6
Light source: mercury arc lamp
Filters can be used to limit exposure wavelengths.
Intensity uniformity has to be better than several % over the collection area.
Needs spectral exposure meter for routine calibration due to aging.
High pressure Hg-vapor lamps
Order $1000, lasts 1000 hours.
Traditionally Hg vapor lamps have been used which generate many spectral lines from a high intensity plasma inside a glass lamp.
Electrons are excited to higher energy levels by collisions in the plasma, and photons are emitted when the energy is released. (electron effective temperature 40000K in a plasma!! )
g line =436 nm
i line =365 nm
(used for 0.5μm and 0.35μm lithography generation)
Notes: Similar to fluorescent lamp, but that is LOW pressure.

## Slide 7
Light source: excimer laser
Decreasing feature size (to <0.35m) requires shorter .
Brightest sources in deep UV are excimer lasers.
Excimer laser:
In excimer lasers, two elements, e.g. a noble gas and a halogen (from a halogen containing compound), which can react and “bind” together only in the excited state but not in their ground states, are present.
Providing energy will therefore drive the reaction, creating the excimer.
When the excitation energy is removed, the excimer dissociates and releases the energy at the characteristic wavelength.
A pulsed excitation is used to repeat the process.
KrF  = 248 nm (used for 0.25μm lithography generation)
ArF  = 193 nm (currently used for 45nm node/generation production)
Eximer = Excited dimer
Xe* + Cl2  XeCl* + Cl
XeCl*  XeCl + DUV
DUV = deep UV, 308nm for XeCl laser
XeCl  Xe + Cl
Here “*” means excited state

## Slide 8
Light sources: summary
CD: critical dimension
Note: the numbers in the two tables are different, so they must be for different systems

## Slide 9
Photomask
Types:
Photographic emulsion on soda lime glass (cheap).
Fe2O3 on soda lime glass (no longer in use?).
Cr on soda lime glass and on quartz glass (most popular).
  (Quartz has low thermal expansion coefficient and low absorption of light, but more expensive; needed for deep UV lithography).
Transparency by laser printer, more and more popular for MEMS (resolution down to few m with a 20000 dpi printer, very cheap).
Polarity:
Light-field, mostly clear, drawn feature is opaque.
Dark-field, mostly opaque, drawn feature is clear.
Three potential mask improvements:
Pellicle, antireflective coatings, phase-shift masks.
(we want 100% transmission, no reflection)
Light-field photomask

## Slide 10
The particle on the pellicle surface is outside of optical focal range.
Antireflective coatings
Pellicle film
Chrome pattern
Depth of focus
Mask material
Reticle
Pellicle film
Frame
Chrome pattern
Pellicle on a reticle (IC word for mask)
Pellicle: (used only for IC manufacturing where yield is important)
A thin coating of transparent material similar to Mylar is stretched over a cylindrical frame on either side of the mask.
The frame stands off the membrane at a distance of 1 cm from the surface of the mask.
Purpose of pellicle is to ensure that particle that fall in the mask are kept outside of the focal plane of the optical system.

## Slide 11
Photomask (Cr pattern on quartz) fabrication
(Cr is 100nm thick)
Remove the resist.
Laser beam writing:
Similar to photolithography, but use a focused laser beam.
It is a direct-write technique - no mask is needed.
Resolution down to a few 100nm, cheaper than electron-beam writing.

## Slide 12
Photomask fabrication by electron beam lithography
12. Finished
quartz

## Slide 13
Mask fabrication by photo-reduction (demagnification)
Minimum feature size 1-5m
This is similar to photography, where image is reduced onto the negative film.

## Slide 14
Mask fabrication by photo-reduction
The beginning “artwork” is huge (close to 1 meter) that can be made easily by printing, the final photomask is only order 1 inch with m feature size on it.

## Slide 15
Mask to wafer alignment
Alignment mark on wafer created from prior processing step.
Alignment mark on mask, open window in Cr through which mark on wafer can be seen.
3 degrees of freedom between mask and wafer: x, y,  (angle)
Use alignment marks on mask and wafer to register patterns prior to exposure.
Modern steppers use automatic pattern recognition and alignment systems, which takes 1-5 sec to align and expose.
Normally requires at least two alignment mark sets on opposite sides of wafer or stepped region, and use a split-field microscope to make alignment easier.
Use vernier for more precise alignment

## Slide 16
Alignment problems: thermal expansion
ΔTm, ΔTsi = change of mask and wafer temperature.
m, si = coefficient of thermal expansion of mask & silicon.
Alignment mark on mask
Pattern on wafer for alignment
For example, for thermal expansion of 2ppm/oC (silicon 2.6, fused silica/quartz 0.5 ppm/oC), assume temperature change of 1oC, then the distance between two features separated by 50mm will change by 2ppm or 100nm, which is too large for IC production but OK for most R&D.

## Slide 17
Introduction and application.
Light source and photomask, alignment.
Photolithography systems.
Resolution, depth of focus, modulation transfer function.
Other lithography issues: none-flat wafer, standing wave...
Photoresist.
Resist sensitivity, contrast and gray-scale photolithography.
Step-by-step process of photolithography.
Chapter 5 Lithography
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 18
Three basic methods of wafer exposure
High resolution. But mask wear, defect generation.
Less mask wear /contamination, less resolution (depend on gap).
Fast, simple and inexpensive, choice for R&D.
No mask wear/contamination, mask de-magnified 4 (resist features 4 smaller than mask). Very expensive, mainly used for IC industry.
Figure 5.3

## Slide 19
Contact/proximity exposure system (called mask aligner)
4 objectives of optical exposure system
Collect as much of radiation
Uniform radiation over field of exposure
Collimate and shape radiation
Select exposure wavelength
Hard to maintain contact or constant gap when wafer/mask is not even/flat.
Resolution (half-period for grating pattern) is given by:
g is gap (=0 for contact), t is resist thickness, and  is wavelength.

## Slide 20
Single field exposure, includes: focus, align, expose, step, and repeat process
UV light source
Reticle (may contain one or more die in the reticle field)
Shutter
Wafer stage controls position of wafer in
X, Y, Z, 
Projection lens (reduces the size of reticle field for presentation to the wafer surface)
Shutter is closed during focus and alignment and removed during wafer exposure
Alignment laser
Stepper (step and repeat system)
Die-by-die exposure
Feature size (typically) 4 reduction

## Slide 21
Illuminator optics
Beam line
Excimer laser (193 nm ArF )
4:1 Reduction lens
Wafer transport system
Reticle stage
Auto-alignment system
Wafer stage
Reticle library
(SMIF pod interface)
Step and scan (stepper) exposure system: 193nm
Optical train for an excimer laser stepper
193nm stepper systems are used today for IC manufacturing.
Excimer laser: light is in pulses of 20ns duration at a repetition rate of a few kHz.
About 50 pulses are used for each exposure.

## Slide 22
Step and scan (stepper) exposure system: 157nm
However, 157nm was not used for production and will never be used, because it needs expensive vacuum (air absorb 157nm), and lens materials (CaF2) have much higher thermal expansion coefficient than quartz (quartz absorb 157nm, thus unsuitable).