## Slide 1
Introduction and application.
Light source and photomask, alignment.
Photolithography systems.
Resolution, depth of focus, modulation transfer function.
Other lithography issues: none-flat wafer, standing wave...
Photoresist.
Resist sensitivity, contrast and gray-scale photolithography.
Step-by-step process of photolithography.
Chapter 5 Lithography
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Light diffraction through an aperture on mask

## Slide 3
Three basic methods of wafer exposure
High resolution. But mask wear, defect generation.
Less mask wear /contamination, less resolution (depend on gap).
Fast, simple and inexpensive, choice for R&D.
No mask wear/contamination, mask de-magnified 4 (resist features 4 smaller than mask). Very expensive, mainly used for IC industry.

## Slide 4
For g=10m, =365nm
Wmin  2 m
Near field/Fresnel diffraction for contact/proximity exposure
Interference effects and diffraction result in “ringing” and spreading outside the aperture.
Edges of image rise gradually (not abrupt) from zero.
Intensity of image oscillates about the expected intensity.
Oscillations decay as one approaches the center of the image.
The oscillations are due to constructive and destructive interference of Huygen’s wavelets from the aperture in the mask.
When aperture width is small, the oscillations are large
When aperture width is large, the oscillations rapidly die out, and one approaches simple ray tracing when aperture >> .
(t is resist thickness)
Near field:
(g is gap)
Figure 5.14

## Slide 5
Far field: W2 << (g2+r2)1/2, r is position on the wafer.
Sharp maximum intensity at x=0, and intensity goes through 0 at integer multiples of one-half number.
Far field/Fraunhofer diffraction for projection exposure
Far field
Near field
Figure 5.15

## Slide 6
UV
0
1
2
3
4
1
2
3
4
Lens
Quartz
Chrome
Diffraction patterns
Mask
Lens capturing diffracted light
Large lens captures more diffracted light, and those higher order diffracted light carries high frequency (detail of fine features on mask) information.

## Slide 7
Numerical aperture of a lens

Numerical aperture (NA) of an optical system is a measure of the ability of the lens to collect light.
NA  nsin, n is refractive index for the medium at the resist surface (air, oil, water).
For air, refractive index n=1, NA = sin  (d/2)/f  d for small .

## Slide 8
Exposure light
Lens NA
Pinhole masks
Image results
(not in same scale)
Diffracted light
Good
Bad
Poor
Effect of numerical aperture on imaging
Large lens
Small lens

## Slide 9
Light diffraction through a small circular aperture
Light intensity on image plate
A point image is formed only if 0, f 0 or d.
“Airy disk”
http://en.wikipedia.org/wiki/Airy_disk
Figure 5.7 Image intensity of a circular aperture in the image plane.
Figure 5.6 Qualitative example of a small aperture being imaged.

## Slide 10
Resolved images
Unresolved images
Lord Rayleigh
Rayleigh criteria for resolution
Rayleigh suggested that a reasonable criterion for resolution is that the central maximum of each point source lie at the first minimum of the Airy pattern.
Strictly speaking, this and next slides make sense only for infinitely far (>>f) objects, like eye. Fortunately, 4x reduction means far object, and near (near focal plane) image.
Figure 5.8

## Slide 11
Rayleigh criteria for resolution R
S1
S2
S1
S2
S1
S2
To increase resolution, one can:
Increase NA by using large lens and/or immersion in a liquid (n>1).
Decrease k1 factor (many tricks to do so).
Decrease  (not easy, industry still insists on 193nm).
K1 factor has no well-defined physical meaning.
It is an experimental parameter, depends on the lithography system and resist properties.

## Slide 12
Effect of imaging/printing conditions
Annular means an “off-axis illumination” method, which is one trick to decrease k1.
EUV: extreme UV, here wavelength 13.5nm. Immersion means exposure in water.

## Slide 13
A small aperture was used to ensure the foreground
stones were as sharp as the ones in the distance.
What one need here is a telephoto lens at its widest aperture.
Depth of focus (DOF)
DOF for photography
Small DOF
(background blurred)
Large DOF
Focal point
DOF
DOF is the range in which the image is in focus and clearly resolved.

## Slide 14
Rayleigh criteria for depth of focus (DOF)
Rayleigh criteria: the length of two optical paths, one on-axis, one from lens edge or limiting aperture, not differ by more than /4.
For small 
O
A
B
C
On axis, optical path increased by OC-OB=.
From edge, increased by AC-AB=DC=cos.
At point B (focal point), two branches have equal path.
D
Again, like the case of resolution, we used k2 factor as an experimental parameter. It has no well-defined physical meaning.
Figure 5.9

## Slide 15
Depth of focus for projection photolithography
It can be seen that larger NA gives smaller depth of focus!
This is also true for camera. A cheap camera takes photos that are always in focus no matter where the subject is, this is because it has small lenses.
This of course works against resolution where larger NA improves this property.
In order to improve resolution without impacting DOF too much, λ has been reduced and “optical tricks” have been employed.
Large lens (large NA), small DOF
Small lens (small NA), large DOF

## Slide 16
Optimal focal plane in photolithography
Light should be focused on the middle point of the resist layer.
In IC, DOF is << 1m, hard to focus if wafer is not super flat.
People talks more of resolution, but actually DOF can often be a bigger problem than resolution.
For example, a 248nm (KrF) exposure system with a NA = 0.6 would have a resolution of 0.3μm (k1 = 0.75) and a DOF of only  ±0.35μm (k2 = 0.5).
Focal plane
Depth of focus

## Slide 17
Modulation transfer function is another useful concept.
It is a measure of image contrast on resist.
Modulation transfer function (MTF)
Figure 5.10

## Slide 18
MTF and spatial coherence
Usually MTF > 0.5 is preferred.
It depends on , light source size (coherency), and optical system.
It certainly also depends on feature size (or period for a grating pattern).
Spatial coherence of light source
Point source is coherent
Partially
coherent
Coherent light will have a phase to space relationship.
Incoherent light or light with only partial coherence will have wave-fronts that are only partially correlated.
Spatial coherence S is an indication of the angular range of light waves incident on mask, or degree to which light from source are in phase.
Small S is not always good (see next slide).
Figure 5.12
Plane wave

## Slide 19
MTF and spatial coherence
For a source with perfect spatial coherence S=0, MTF drops abruptly at Rayleigh criterion W=half pitch=R=k1/NA.
Large S is good for smaller features, but bad for larger ones.
Trade-off is made, and industry chooses S=0.5-0.7 as optimal.
MTF vs. diffraction grating period on mask.
W = line width = space width of the grating.
X-axis of the plot: spatial frequency =1/(2W), normalized to Rayleigh criterion cutoff frequency 0=1/R=NA/(0.61).
2W
Grating photomask
Large features Smaller features
(similar to Figure 5.13)

## Slide 20
Introduction and application.
Light source and photomask, alignment.
Photolithography systems.
Resolution, depth of focus, modulation transfer function.
Other lithography issues: none-flat wafer, standing wave...
Photoresist.
Resist sensitivity, contrast and gray-scale photolithography.
Step-by-step process of photolithography.
Chapter 5 Lithography
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 21
Exposure on patterned none-flat surface
This leads to random reflection/proximity scattering, and over or under-exposure.
Proximity scattering
Both problems would disappear if there is no reflection from substrate.

## Slide 22
Exposure on patterned none-flat surface
To reduce the problem, one can:
Use absorption dyes in photoresist, thus little light reaches substrate for reflection.
Use anti-reflection coating (ARC) below resist.
Use multi-layer resist process (see figure below)
  thin planar layer for high-resolution imaging (imaging layer).
  thin develop-stop layer, used for pattern transfer to 3 (etch stop).
  thick layer of hardened resist (planarization layer).

## Slide 23
Surface reflection and standing wave
Resist is partially reflective, so some light reaches resist bottom and is reflected.
Constructive and destructive interference between incident and reflected light results in a periodic intensity distribution across the resist thickness.
With change in exposure (light intensity) comes change in resist dissolution rate, leading to zigzag resist profile after development.
Use of anti-reflecting coating (ARC) eliminates such standing wave patterns.
Post exposure bake also helps by smoothing out the zigzag due to resist thermal reflow.
(Also due to reflection, a metal layer on the surface will require a shorter exposure than exposure over less reflective film.)
Figure 5.24

## Slide 24
Photoresist
/2nPR
Substrate
Overexposure
Underexposure
Standing wave effect on photoresist
Is this a positive or negative resist?
nPR is refractive index of photoresist

## Slide 25
(m0, 2, 4, 6…)
Position of minimum and maximum intensity
Maximum when optical path difference between incident and reflected beams is m.
There may be a 180o phase shift when light is reflected at the resist/substrate interface, thus it is minimum (rather than maximum) when x=d.
Positive resist