## Slide 1
SiO2 properties and applications.
Thermal oxidation basics.
Manufacturing methods and equipment.
Measurement methods.
Deal-grove model (linear parabolic model).
Thin oxide growth, dependence on gas pressure and crystal orientation
Cl-containing gas, 2D growth, substrate doping effect .
Interface charges, dopant redistribution.
Si(s) + O2(g)  SiO2(s)
Chapter 6 Thermal oxidation and the Si/SiO2 interface
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Properties of thermally grown SiO2
It is amorphous.
Stable, reproducible and conformal SiO2 growth
Melting point: 1700C
Density: 2.21 g/cm3 (almost the same as Si that is 2.33 g/cm3)
Crystalline SiO2 [Quartz] = 2.65gm/cm3
Atomic density: 2.31022 molecules/cm3
(For Si, it is 51022 atoms/cm3)
Refractive index: n=1.46
Dielectric constant: =3.9 (why not =n2?)
Excellent electrical insulator: resistivity  > 1020 cm, energy gap Eg=8-9 eV.
High breakdown electric field: >107 V/cm
Conformal growth

## Slide 3
The perfect interface between Si and SiO2 is one major reason why Si is used for semiconductor devices (instead of Ge…)
Thermal oxide (amorphous)
Si substrate
(single crystal)
The Si/SiO2 interface

## Slide 4
STI
Application of SiO2 in IC industry
Very good etching selectivity between Si and SiO2 using HF
STI: shallow trench isolation

## Slide 5
Diffusion mask for common dopants
SiO2 can provide a selective mask against
diffusion at high temperatures. (DSiO2 << Dsi)
Oxides used for masking are 0.5-1μm thick.
SiO2 masks for B and P
(not good for Ga)
Can also be used for mask against ion implantation
Diffusion time (hr)
Mask thickness (m)

## Slide 6
Gate oxide, only 0.8nm thick!
As insulation material between interconnection levels and adjacent devices
Use of oxide in MOSFET
LOCOS: local oxidation isolation; STI: shallow trench isolation

## Slide 7
Local Oxidation of Si (LOCOS)
Fully recessed process attempts to minimize bird’s peak.

## Slide 8
For nanofabrication: oxidation sharpening for sharp AFM tips or field emitters for display
Si
SiO2
Ding, “Silicon Field Emission Arrays With Atomically Sharp Tips: Turn-On Voltage and the Effect of Tip Radius Distribution”, 2002.
Field emission display (FED)

## Slide 9
Oxide Structure
Basic structure of silica: a silicon atom tetrahedrally bonds to four oxygen atoms
The structure of silicon-silicon dioxide interface: some silicon atoms have dangling bonds.
Amorphous tetrahedral network
非桥联氧
桥联氧
Bridging oxygen Non-bridging

## Slide 10
Single crystal (quartz)
2.65 g/cm3
Amouphous (thermal oxide). 2.21 g/cm3
Oxide Structure

## Slide 11
SiO2 properties and applications.
Thermal oxidation basics.
Manufacturing methods and equipment.
Measurement methods.
Deal-grove model (linear parabolic model).
Thin oxide growth, dependence on gas pressure and crystal orientation
Cl-containing gas, 2D growth, substrate doping effect .
Interface charges, dopant redistribution.
Chapter 6 Thermal oxidation and the Si/SiO2 interface
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 12
Dry and wet oxidation
Dry oxidation: Si(s) + O2(g)  SiO2(s); Wet/steam oxidation: Si(s) + 2H2O(g)  SiO2(s) + 2H2(g)
Both typically 900-1200°C, wet oxidation is about 10 faster than dry oxidation.
Dry oxide: thin 0.05-0.5m, excellent insulator, for gate oxides; for very thin gate oxides, may add nitrogen to form oxynitrides.
  Wet oxide: thick <2.5 m, good insulator, for field oxides or masking. Quality suffers due to the diffusion of the hydrogen gas out of the film, which creates paths that electrons can follow.
Room temperature Si in air creates “native oxide”: very thin 1-2nm, poor insulator, but can impede surface processing of Si.
Volume expansion by 2.2 (=1/0.46), so SiO2 film has compressive stress.
= 0.46
Si wafer
Xox is final oxide thickness

## Slide 13
SiO2 properties and applications.
Thermal oxidation basics.
Manufacturing methods and equipment.
Measurement methods.
Deal-grove model (linear parabolic model).
Thin oxide growth, dependence on gas pressure and crystal orientation
Cl-containing gas, 2D growth, substrate doping effect .
Interface charges, dopant redistribution.
Chapter 6 Thermal oxidation and the Si/SiO2 interface
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 14
Thermal silicon oxidation methods
A three-tube horizontal furnace with multi-zone temperature control
Vertical furnace
(not popular)
Wet oxidation using H2 and O2 is more popular (cleaner) than using H2O vapor.

## Slide 15
The tubular reactor made of quartz or glass, heated by resistance.
Oxygen or water vapor flows through the reactor and past the silicon wafers, with a typical velocity of order 1cm/s.
Thermal oxidation equipment

## Slide 16
Clean the wafers (RCA clean, very important)
Put wafers in the boat
Load the wafers in the furnace
Ramp up the furnace to process temperature in N2 (prevents oxidation from occurring)
Stabilize
Process (wet or dry oxidation)
Anneal in N2. Again, nitrogen stops oxidation process.
Ramp down
Thermal oxidation in practice

## Slide 17
SiO2 properties and applications.
Thermal oxidation basics.
Manufacturing methods and equipment.
Measurement methods (mechanical, optical, electrical).
Deal-grove model (linear parabolic model).
Thin oxide growth, dependence on gas pressure and crystal orientation
Cl-containing gas, 2D growth, substrate doping effect .
Interface charges, dopant redistribution.
Chapter 6 Thermal oxidation and the Si/SiO2 interface
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 18
Oxide etched away by HF over part of the wafer and a mechanical stylus is dragged over the resulting step.
Surface profilometry (Dektak): mechanical thickness measurement
Stylus
Mirror image of stylus
stylus
AFM can also be used for thickness measurement.
(AFM: atomic force microscopy)

## Slide 19
Thickness determination by looking the color
Oxide thickness for constructive interference (viewed from above =0o) Xo=k/2n, n=1.46, k=1, 2, 3…
Our eye can tell the color difference between two films having 10nm thickness difference.
Film thickness (nm)
Relative illumination intensity

## Slide 20
After quarter wave plate, the linear polarized light becomes circular polarized, which is incident on the oxide covered wafer.
The polarization of the reflected light, which depends on the thickness and refractive index (usually known) of the oxide layer, is determined and used to calculate the oxide thickness.
Multiple wavelengths/incident angles can be used to measure thickness/refractive index of each film in a multi-film stack.
Optical thickness measurement: ellipsometry
Very accurate (1nm accuracy)

## Slide 21
Electrical thickness measurement: C-V of MOSFET
Substrate is N-type. Electron is majority carrier, hole is minority carrier.
Accumulation: positive gate voltage attracts electrons to the interface.
Depletion: negative gate bias pushes electrons away from interface. No charge at interface. Two capacitance in series.
Inversion: further increase (negative) gate voltage causes holes to appear at the interface.
Small AC voltage is applied on top of the DC voltage for capacitance measurement.

## Slide 22
P-type substrate here
(previous slide N-type)
Effect of frequency for AC capacitance measurement
At/after inversion:
For low frequency, (minority) charge generation at the interface can follow the AC field to balance the charge at the gate, so Cinv=Cox.
For high frequency, the gate charge has to be balanced by the carrier deep below the interface, so Cinv-1 = Cox-1 + CSi-1.
Deep depletion: for high scanning speed (the DC voltage scan fast into large positive voltage), depletion depth Xd must increase to balance the gate charge.
Parameter from C-V measurement:
Dielectric constant of Si & SiO2
Capacitor area
Oxide thickness
Impurity profile in Si
Threshold voltage of MOS capacitor