## Slide 1
Introduction and application.
Dopant solid solubility and sheet resistance.
Microscopic view point: diffusion equations.
Physical basis for diffusion.
Non-ideal and extrinsic diffusion.
Dopant segregation and effect of oxidation.
Manufacturing and measurement methods.
Chapter 7 Dopant Diffusion
NE 343: Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo; http://ece.uwaterloo.ca/~bcui/
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 2
Interstitial
Substitutional
Impurities diffuse by interstitial：O, Au, Ag, Fe, Cu, Ni, Zn, Mg, Li, H.
Impurities that diffuse by substitutional: As, Al, Ga, Sb, Ge.
Usually there must be a vacancy nearby for this diffusion to happen.
Physical basis for diffusion

## Slide 3
Diffusion mechanisms in Si: interstitial
No Si native point defect required
Very fast diffusion
“Hopping” frequency:
Energy barrier Ei: 0.6-1.2eV
Vibration frequency 0: 1012-1014/sec.
Ei

## Slide 4
Thermal-equilibrium values of Si neutral interstitials and vacancies at diffusion temperatures << doping concentration of interest (1015 –1020/cm3).
Diffusivity of Si interstitials and Si vacancies >> diffusivity of dopants.
Interstitials and vacancies in Si
Vacancy concentration:
Probability of a site to be vacant:

## Slide 5
Si native point defects required (Si vacancy and Si interstitials); Examples: B, P, As, Sb.
Diffusion mechanisms in Si: substitutional and interstitialcy
b) Interstitialcy diffusion
a) Substitutional diffusion
Si atom
Vacancy
Substitutional impurity atom
“Hopping” frequency:
Es: 3-4eV

## Slide 6
Diffusion mechanisms in Si: kick out and Frank Turnbull
(continued from previous slide)
c) Kick out diffusion
d) Frank Turnbull diffusion
Continued from previous slide
(Si native point defects required…)
Very slow diffusion

## Slide 7
Diffusivity comparison
108 times higher!!
Figure 4-8 Diffusivities of various species in silicon. Aus refers to gold in substitutional form (on a lattice site); AuI to gold in an interstitial site. The silicon interstitial (I) diffusivity is also shown, and the grey area representing the I diffusivity indicates the uncertainty in this parameter.

## Slide 8
Introduction and application.
Dopant solid solubility and sheet resistance.
Microscopic view point: diffusion equations.
Physical basis for diffusion.
Non-ideal and extrinsic diffusion.
Dopant segregation and effect of oxidation.
Manufacturing and measurement methods.
Chapter 7 Dopant Diffusion
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 9
Field also leads to diffusion of substrate dopants that are negatively charged for P-type.
Electric field effect: non-intrinsic/extrinsic diffusion
Fick’s Laws: only valid for diffusion under special conditions.
When the doping is higher than ni, -field effects become important .
The field comes from higher mobility of electrons and holes compared to dopant atoms.
Carries move faster than dopants, until an equilibrium is attained due to the electric field that slows down carrier and speeds up dopant.
N-type dopants are positively charged.
Figure 7-25, P406
Figure 7-26

## Slide 10
Electric field () effect on dopant diffusion
Total dopant flux contains two parts, drift velocity v=.
For n-type doping,  is potential.
Therefore.
Einstein relation.
(you are not required to know well those equations)
Here  is for dopant atom, not for carrier (e, h)

## Slide 11
Concentration dependent diffusion
At high doping concentrations, the Fick’s equation must be solved numerically since Dconstant.
The dash line show the erfc profiles.
The solid lines are numerical simulations, which agree with experimental results.
Those box-like (steep) doping profile is often desirable.
Figure 7-28

## Slide 12
Introduction and application.
Dopant solid solubility and sheet resistance.
Microscopic view point: diffusion equations.
Physical basis for diffusion.
Non-ideal and extrinsic diffusion.
Dopant segregation and effect of oxidation.
Manufacturing and measurement methods.
Chapter 7 Dopant Diffusion
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 13
Dopant segregation
Dopants segregate coefficient k0.
0.3 for Boron, B
10 for Arsenic, As
10 for Antimony, Sb
10 for Phosphorus, P
Oxidation of a uniformly doped boron substrate depletes the boron into the growing SiO2.
Whereas N-type dopants tend to pile-up near the interface.
Figure 7-31, P416

## Slide 14
Interfacial dopant pile-up during oxidation
Dopants may also segregate to an interface layer, perhaps only a monolayer thick.
They are not active (do not contribute electrons/holes).
This may consume up to 50% of the dose in a shallow layer.
Figure 7-32

## Slide 15
Oxidation enhanced (OED)/retarded diffusion (ORD)
Si interstitials created by oxidation, which recombine with vacancies to reduce its concentration.
Oxidation injects interstitials into Si.
Because B and P diffuse mainly by an interstitial process, their diffusion is enhanced by oxidation.
dXox/dt is oxidation rate
But Sb is large and diffuses only by vacancies, so its diffusion is suppressed/retarded.
P419

## Slide 16
Introduction and application.
Dopant solid solubility and sheet resistance.
Microscopic view point: diffusion equations.
Physical basis for diffusion.
Non-ideal and extrinsic diffusion.
Dopant segregation and effect of oxidation.
Manufacturing and measurement methods.
Chapter 7 Dopant Diffusion
NE 343 Microfabrication and thin film technology
Instructor: Bo Cui, ECE, University of Waterloo
Textbook: Silicon VLSI Technology by Plummer, Deal and Griffin

## Slide 17
Diffusion furnace: horizontal
Temperature control in 3 to 5 zones by spike thermocouples.
Diffusion tube and boat made from SiO2, SiC…
Horizontal furnaces were the diffusion work horses up to 200 mm wafers

## Slide 18
Vertical furnace for 300mm wafers. Close view into three tubes
Vertical furnaces are used for 200mm and above wafers.
Diffusion furnace: vertical

## Slide 19
Open furnace tube systems
  Solid source in platinum source boat
  Liquid Source - carrier gas passing through bubbler
  Gaseous impurity source
Gas source
Liquid source
Solid source
Spin-on glass
Note: for drive-in, a capping layer (SiO2…) is often used to prevent out-diffusion into air.
Diffusion methods

## Slide 20
Gas source doping, very toxic gases
Silane and dichlorosilane used for polysilicon deposition

## Slide 21
Liquid source doping
Container of the liquid is immersed in a constant temperature bath to produce a known vapor pressure of the dopant above the liquid surface.
An inert gas such as N2 is injected into the bubbler.
Partial pressure of dopant in furnace is controlled by
  Bath temperature
  Gas pressure above liquid
  Ratio of flow through bubbler to the sum of all other flows into furnace.
Usually an O2 source is supplied to react with the dopant gas.
Disadvantage of liquid source:
Source is corrosive.
Bubblers must be pressurized and have been known to explode.
Sensitive to bubbler temperature change.
Danger of forming insoluble silicon compounds at wafer surface that are invisible, but are extremely undesirable.

## Slide 22
Solid source doping
Another way is to use discs that are side-by-side to the Si wafer.
For example, for diffusing p-type layers in Si, boron nitride (BN) disc is used.
When oxidized at 750-1100℃, a thin film of B2O3 forms at the surface.
In presence of H2, the volatile compound HBO2 forms and diffuses to wafer surface where a borosilicate glass in formed.
This glass serves as the boron source for diffusion into the substrate.
No carrier gas needed, but protected under N2 or Ar gas.

## Slide 23
Spin on glass doping
Spin-coat an oxide on the wafer (room temperature).
Bake at 200oC for 15min to remove solvent.
Effectively, the film can be considered as a mixture of SiO2 and dopant oxide.
Then diffuse into Si at high temperature.
Good for many types of dopant, with a wide range of dose.
This is finite source, whereas gas/liquid/solid are infinite source.
Sources:
As: arsenosilica
Sb: antimonysilica
B: borosilica
P: phosphorosilica

## Slide 24
Diffusion system: Boron
Surface reaction:
Solid sources: boron nitride (BN) and trimethylborate (TMB).
TMB has high vapor pressure at room temperature,
so placed outside of furnace.
One can also use BN wafers, pass O2, 900oC.
Liquid sources: boron tribromide BBr3.
Gaseous sources: diborane B2H6.
4BN + 3O2  2B2O3 + 2N2

## Slide 25
Diffusion system: Phosphorus
Surface reaction:
Solid sources: (can be made into wafers like BN, but not popular)
Phosphorus pentoxide
Ammonium monophosphate NH4H2PO4
Ammonium diphosphate (NH4)2H2PO4
Liquid source: phosphorus oxychloride POCl3
Gaseous source: phosphine PH3.

## Slide 26
Diffusion system: Arsenic & Antimony
Arsenic surface reaction:
Solid sources: possible, low surface concentrations.
Gaseous source: arsine AsH3.
Ion implantation is normally used for deposition.
Antimony surface reaction:
Liquid source: antimony pentachloride Sb3Cl5.
Ion implantation is normally used for deposition.

## Slide 27
Measurement methods
Sheet resistance measurement using four-point probe.
p-n junction staining for junction depth. (see below, left)
Capacitance-voltage measurement for dopant concentration
Secondary Ion Mass Spectroscopy, SIMS, for impurity concentration
Spreading resistance measurement. (see below, right)
a
Metal needle point-contact with the semiconductor, resistance mainly comes from the volume near the needle tip.
a: effective contact radius
K: empirical parameter

## Slide 28
Secondary Ion Mass Spectroscopy, SIMS
Measured by SIMS